## Slide 1: Tank Leakage Before Coating for FY (2022- 23)
Sr.No | Month | Issue | Root Cause | Action Plan | Trg Date | Resp. | Status
1 | May-22 | Tank Leakage | Pipe Welding doing not proper | Inform to Tank fabrication incharge and rejection data share | 22.05.22 | MPPL - 5/25 | Done
2 | Jun-22 | Tank Leakage | Centre Welding doing not Proper | Inform to Tank fabrication incharge and rejection data share | 18.06.22 | MPPL - 5/25 | Done
3 | Jul-22 | Tank Leakage | Welding Mchine Working not Proper | Inform to Tank fabrication incharge and rejection data share | 19.07.22 | MPPL - 5/25 | Done
4 | Aug-22 | Tank Leakage | Sol. Qube leakage testing fixture non availability | Leakage testing fixture repaired | 11.08.22 | MPPL - 5/25 | Done
5 | Sep-22 | Tank Leakage | Pipe welding doing not proper | Inform to tank fabrication incharge and rejection data share | 12.09.22 | MPPL - 5/25 | Done
Chart: 
| 44703 | 44735 | 44766 | 44798 | 44830
Total Qty Checked | 1937 | 3974 | 4691 | 7362 | 14025
Total Ok | 1860 | 3791 | 4546 | 7148 | 13733
Total Rejection | 77 | 183 | 145 | 214 | 292
Target (%) | 1 | 1 | 1 | 1 | 1
% Of Rejection | 3.9752 | 4.6049 | 3.091 | 2.9068 | 2.082

## Slide 2: Tank Coating Rejection for FY (2022 –23)
Sr.No | Month | Issue | Root Cause | Action Plan | Trg Date | Resp. | Status
1 | July - 22 | Pin Hole | 1- Out of 6 Robotics gun 3 gun charging was not up to mark 2- Oven temperature | 1- Gun replaced 2- TTR done & observed OK | 12.06.22 | Prod. | Done
Chart: 
| 44734 | 44765 | 44797 | 44829 | 44860
Total Check Qty | 4669 | 2560 | 4485 | 13731 | 10335
Total Ok Qty | 4169 | 2360 | 4285 | 13131 | 9935
Total Rejection Qty | 500 | 200 | 200 | 600 | 400
Target(%) | 2.5 | 2.5 | 2.5 | 2.5 | 2.5
Rej(%) | 10.7089 | 7.8125 | 4.4593 | 4.3697 | 3.8703

## Slide 3: Tank Leakage After Coating For FY (2022 – 23)
Sr.No | Month | Issue | Root Cause | Action Plan | Trg Date | Resp. | Status
1 | May-22 | Element Leakage | Less Heating temperature & time to dry Silicon compound | Given temp. & time as per requirement & Follow WI | 15.05.22 | Jai Durga | Done
2 | Jun-22 | Element Leakage | T/S and C/O pocket not proper Welding | Inform to Supplier and share Rejection Data. Given training to operator for use silicon. | 14.06.22 | Jai Durga | Done
Chart: 
| 44703 | 44735 | 44766 | 44798 | 44830
Total Qty Checked | 292 | 2318 | 6701 | 7978 | 11265
Total Ok | 284 | 2275 | 6632 | 7900 | 11209
Total Rejection | 8 | 43 | 69 | 78 | 56
Target (%) | 0.5 | 0.5 | 0.5 | 0.5 | 0.5
% Of Rejection | 2.7397 | 1.855 | 1.0297 | 0.97769 | 0.49711